]

Development and Application of Potentially Important Jute

Geo-textiles

(CFC/IJSG/21)

National Jute Board (PEA)

Project Management Unit (PMU)

75C, Park Street, 6th Floor

Kolkata – 700 016

Phone No.: (033) 2226 7534, (033) 4064 6316

64995824 / 25 / 26 / 27 /28 / 33 / 34

Fax NO. (033) 2226 7535

E-mail: cfcijsg21@gmail.com / jutegeotech@gmail.com

Website: www.jutegeotech.com

##### INTRODUCTION

JUTE GEOTEXTILE (JGT) IS AN EMERGING ENGINEERING PRODUCT WITH APPLICATION-POTENTIAL IN MANY AREAS OF CIVIL ENGINEERING FACED WITH SOIL RELATED PROBLEMS. THE PRODUCT HAS ALREADY BEEN SUCCESSFULLY TRIED IN PROTECTION OF BANKS OF RIVERS AND CANALS, MANAGEMENT OF SLOPES, STRENGTHENING OF ROADS, CONTROLLING OF SUBSIDENCE OF RAILWAY TRACKS, STABILISING EMBANKMENTS & OVERBURDEN DUMPS IN MINES. CONTINUING RESEARCH ON JGT IS OPENING UP POTENTIAL OF THE PRODUCT IN NEW AREAS LIKE FLY ASH STABILISATION.

THE BIGGEST ADVANTAGE OF JGT IS ITS EASY AVAILABLITY, ECONOMIC PRICE-RANGE (MUCH LOWER THAN THE SYNTHETIC AND OTHER NATURAL VARIETIES) AND ECO-COMPATIBILITY. BESIDES, JGT CAN BE TAILOR-MADE AS PER END-USERS’ TECHNICAL REQUIREMENTS LIKE POROMETRY, PERMITTIVITY, STRENGTH AND OTHER PARAMETERS.

THIS LITERATURE PROVIDES THE INTERESTED END-USERS, ENGINEERS AND CONSULTANTS WITH TECHNICAL SPECIFICATIONS OF STANDARD JGT. THIS WILL ENABLE THE USERS TO SELECT THE RIGHT TYPE OF JGT FOR A PARTICULAR JOB OR TO DECIDE ON A NON-STANDARD TYPE OF JGT IF WARRANTED.

CONTENTS

| Particulars | Page No |
| --- | --- |
| Jute Geotextiles for Control of Surface Soil Erosion by rain and wind. | 5- 6 |
| Jute Geotextiles for Separation and Filtration. | 7 - 8 |
| Jute Geotextiles for Filtration and Drainage. | 9 - 10 |
| Prefab. Drains for accelarated consolidation of soft soil | 11 - 12 |
| Manufacturers of Jute Geotextiles IN India & Bangladesh | 13 - 16 |
| Organisations involved in promotion of Jute Geotextiles | 17 |

JUTE GEOTEXTILES FOR CONTROL OF

SURFACE SOIL EROSION BY RAIN AND WIND

Open Weave Geo-textile

Indicative Specification

| Properties | 1 | 2 | 3 | Test Method |
| --- | --- | --- | --- | --- |
| Weight (g/m2) | 500 | 600 | 700 | ASTM D5261 |
| Threads/dm (MD x CD) | 6.5 X 4.5 | 8 X 7 | 8 X 8 | IS 1963 |
| Thickness | 4.5 | 5.25 | 5.5 | ASTM D5199 |
| Width (cm) | 122 | 122 | 122 | IS 1954 |
| Open area (%) | 55 | 48 | 40 | - |
| Strength (kN) (MDxCD) | 6.5 x 6.0 | 12 x6 | 14 x 7 | ASTM D4595 |
| Water Holding capacity (%) On dry weight | 500 | 500 | 600 | - |

APPLICATION AREAS

(	SLOPES OF ROAD, RAILWAY AND HILL

(	BRIDGE APPROACH, SLOPE OF RESERVOIRS AND EMABANKMENTS

- STABILISATION OF SAND DUNES ON SEA BEACH, OVER

BURDEN DUMPS OF OPEN CAST MINES AND FLY ASH

DUMPS OF POWER PLANTS.

(	AFFORESTATION IN SEMI-ARID ZONES

JUTE GEOTEXTILS FOR CONTROL OF SURFACE SOIL EROSION BY RAIN AND WIND

Type-1 – 500 gsm

Type-2 - 600 gsm

Type- 3 - 700 gsm

JUTE GEOTEXTILES FOR SEPARATION AND FILTRATION

TYPICAL WOVEN GEOTEXTILES

Indicative Specification

| Properties | Grey (Untreated) | Rot resistance (627 gsm) | Grey (Untreated) | Test Method |
| --- | --- | --- | --- | --- |
| Weight (g/m2) | 627 | 627 | 724 | ASTM D5261 |
| Threads/dm (MD x CD) | 85 x 32 | 85 x 32 | 94 x 39 | IS 1963 |
| Thickness | 1.70 | 1.7 | 1.85 | ASTM D5199 |
| Width (cm) | 100 | 100 | 100 | IS 1954 |
| Strength (kN) (MD x CD) | 20 x 20 | 20 x 20 | 25 x 25 | ASTM D4595 |
| Elongation at break (%) (MD x CD) | 12 x 12 | 12 x 12 | 12 x 12 | ASTM D4595 |
| Pore size (O90) Micron | 300 | 300 | 250 | ASTM D4751 |
| Water permeability at 10 cm water head (I/m2/s) | 40 | 40 | 30 | ASTM D4491 |
| Puncture resistance (kN) | 0.400 | 0.400 | 0.500 | ASTM D4833 |

APPLICATION AREAS

-	CONSTRUCTION OF ROAD & RAILWAY EMBANKMENTS ON SOFT SOIL

-	STRENGTHENING ROAD PAVEMENT

-	RIVER AND CANAL BANK PROTECTION

JUTE GEOTEXTILS FOR SEPARATION AND FILTRATION

20 kN/m, 627 gsm (grey)

20 kN/m, 627 gsm (Rot resistant)

25 kN/m, 724 gsm

JUTE GEOTEXTILES FOR FILTRATION AND DRAINAGE

NON –WOVEN GEOTEXTILES

Indicative Specification

| PROPERTIES | 1 | 2 | Test Method |
| --- | --- | --- | --- |
| Weight (g/m2) at 20% M.R. | 500 | 1000 | ASTM D5261 |
| Thickness (mm) | 4 | 8 | ASTM D5199 |
| Width (cm) | 150 | 150 | IS 1954 |
| Strength (kN/m) [MD x CD] | 4 x 5 | 6 x 7 | ASTM D4595 |
| Elongation at break (%) (MD x CD) | 20 x 25 | 20 x 25 | ASTM D4595 |
| Pore size (O90) Micron | 500 | 300 | ASTM D4751 |
| Co-eff. of water permittivity (m/s) | 3.4 x 10-3 | 3.4 x 10-4 | ASTM D4491 |

APPLICATION AREAS

-	CONSTRUCTION OF CONCEALED RUBBLE DRAINS BY THE SIDE OF ROADS AND RAILWAYS

-	DRAINAGE FOR FILL MATERIALS IN FLYOVERS

PREFAB. DRAINS FOR

ACCELARATED CONSOLIDATION OF SOFT SOIL

PREFABRICATED JUTE DRAIN

Indicative Specification

Material				(  Coir-wicks within jute sheath

Width (mm)			( 100

Thickness (mm)			(  5

Strength (kN)/100 mm	(  45

Pore size (O90) [micron]	( 300

Discharge Capacity

at 50 kPa (I/s)			( 13

APPLICATION AREAS

-	AIRPORTS, WIREHOUSE, CAR PARKS

-	REPAIRING OF ROAD & RAILWAY EMBANKMENT MADE OF

COMPRESSIBLE FILL MATERIAL

PREFAB JUTE DRAINS FOR

ACCELARATED CONSOLIDATION OF SOFT SOIL

Pre- Fabricated Vertical Jute Drain

MANUFACTURERS OF JUTE GEOTEXTILES IN INDIA

| Sl. No. | DW Plain Weave Jute Geotextiles for rural road construction and river bank protection | Open Weave Jute Geotextiles for hill slope protection and soil erosion cotrol |
| --- | --- | --- |
| 1 | Gloster Limited Mr. D. C. Baheti Chairman, IJIRA & Executive Director, Gloster Limited 21 Strand Road, Kolkata – 700 001 (INDIA) Tel (PABX): +91 (33) 2230 9601 (4 Lines) Direct: +91 (33) 2230 2809 / 2230 0451 Mobile: +91 98300 20786 Fax: +91 (33) 2210 6167 / 2231 4222 Email: info@glosterjute.com <dcb@glosterjute.com> Web: www. glosterjute.com | Gloster Limited Mr. D. C. Baheti Chairman, IJIRA & Executive Director, Gloster Limited 21 Strand Road, Kolkata – 700 001 (INDIA) Tel (PABX): +91 (33) 2230 9601 (4 Lines) Direct: +91 (33) 2230 2809 / 2230 0451 Mobile: +91 98300 20786 Fax: +91 (33) 2210 6167 / 2231 4222 Email: info@glosterjute.com <dcb@glosterjute.com> Web: www. glosterjute.com |
| 2 | Reliance Jute Mills (International) Ltd. Mr. V. K. Chaukhani Senior President Marketing Reliance Jute Mills (International) Ltd. Ideal Plaza 11/1 Sarat Bose Road Kolkata – 700 020, India Tel: +91 33 2280 7017 / 7018, 32922619 Dir: 32918764 Res: 32927069 Fax: +91 33 2280 7016 E-mail: mktgho@reliancejute.com Web: www.reliancejute.com | Reliance Jute Mills (International) Ltd. Mr. V. K. Chaukhani Senior President Marketing Reliance Jute Mills (International) Ltd. Ideal Plaza 11/1 Sarat Bose Road Kolkata – 700 020, India Tel: +91 33 2280 7017 / 7018, 32922619 Dir: 32918764 Res: 32927069 Fax: +91 33 2280 7016 E-mail: mktgho@reliancejute.com Web: www.reliancejute.com |
| 3 | Ludlow Jute & Specialities Ltd Mr. Jagdish Prasad Sonthalia Managing Director Ludlow Jute & Specialities Ltd 6, Little Russell Street 4th Floor Kolkata - 700 071 Phone: + 91 33 2283-9081/82/83 Fax: + 91 33 2283-9078/4503 Email: ludlow@giascl01.vsnl.net.in ludlow_123@dataone.in Web: www.ludlowjute.com Shri B. M. Thakkar Resident Director Chengail, Howrah - 711 308 (W.B.) LUDLOW JUTE & SPECIALTIES LTD. 6, Little Russell Street, 4th Floor, Kolkata – 700 071 India Phone No. - 2283 9081/82/83, (D) 2283 4501/02, Fax: 91 33 2283 9078/4503 E-mail: tbhupen@yahoo.co.in ludlow@giascl01.vsnl.net.in; ludlow_123@dataone.in Website: www.ludlowjute.com; | Naffar Chandra Jute Mills Ltd. Mr. D. J. Wadhwa Naffar Chandra Jute Mills Ltd. 2, Cooper Lane, Kolkata – 700 001 Tel: (033) 2237-7880/85, 2225-1050/7924 Fax: (033) 2225-0221, 2236-3754 E-mail: nafa5542@dataone.in , ncjmill@vsnl.net |
| 4 | Birla Corporation Ltd. Shri D. C. Patni Vice-President Birla Corporation Ltd., Unit : Birla Jute Mills, 9/1 R. N. Mukherjee Road Kolkata – 700 001 Tel: (033) 2213-1680/0380 Fax: E-mail : dcpatni@birlacorp.com | Bristi Vinimay Pvt. Ltd. Mr. M. Jain M/s Bristi Vinimay Pvt. Ltd. Unit: Premchand Jute Mills Ltd. 14, Netaji Subhas Road (3rd Floor) Kolkata – 700 001 Fax: 2210-2033 Tel: 3020-3600 Fax: 2210-2033 E-mail: premchandjutemills@hotmail.com |
| 5 | Murlidhar Ratanlal Exports Ltd Shri L. R. Lodha, Executive Director Murlidhar Ratanlal Exports Ltd., Unit : Hastings Jute Mills Kolkata Tel: (033) 2248-9801/9842 Fax: (033) 2230-2260 E-mail: kajaria@jute-india.com, hastings@jute-india.com |  |
| 6 | Hooghly Infrastructure Pvt. Ltd., Shri S. K. Chandra Chief Executive (Works) and Director, Hooghly Infrastructure Pvt. Ltd., Unit : Hukumchand Jute Mill 10, Dr. Rajendra Prasad Sarani (Clive Row) 3rd Floor Kolkata – 700 001 Phone No.: (033) 2242 6064 / 9801 / 9842 / 9790 (H.O.) Fax: 2242 4306 / 4017 1230 / 1245 (033) 2588 8578 / 8062 (Mill) Mobile: 98300 97285 Tel. Fax: 2588 3675 (Mill) Resi: 2588 8569 / 2632 2364 E-mail : hcjm_shipping@rediffmail.com chandra_samir@ rediffmail.com |  |
| 7 | Cheviot Co. Ltd. Mr. N. K. Kejrewal Cheviot Co. Ltd. Magma House 24, Park Street (9th Floor) Kolkata - 700 016 E-mail: cheviot@chevjute.com |  |
| 8 | Shree Gouri Shankar Jute Mills Ltd. Mr. C. S. Chajjer Managing Director 67, Park Street (Ground Floor) Kolkata - 700 016 Mob: 9830971051 E-mail: sgsjml@gmail.com |  |

MANFACTURERS OF JUTE GEOTEXTILES IN BANGLADESH

| SL. No. | DW Plain Weave Jute Geo-textiles for rural road construction and river bank protection | Open Weave Jute Geo-textiles for hill slope protection and soil erosion control |
| --- | --- | --- |
| 1 | BJMC Jute Mills | BJMC Jute Mills |
|  | Bangladesh Jute Mills Corporation Major General Humayun Khaled, psc Chairman Bangladesh Jute Mills Corporation Adamjee Court (Annex-1) Motijheel C/A, Dhaka-1000 Tel.: 88-02-9565514, 9553364. Fax: 88-02-9567508, 9564740 Mob.: 01755-639417 E-mail: khd732@yahoo.com, bjmc.bd@gmail.com Website: www.bjmc.gov.bd Md. Abu Sayed Director (Marketing & RQC) Bangladesh Jute Mills Corporation Adamjee Court (Annex-1) Motijheel C/A, Dhaka-1000 Tel.: 9565519 Fax: 88-02-9567508, 9564740 E-mail: masayed1954@gmail.com bjmc.bd@gmail.com Latif Bawany Jute Mills Ltd. Jyotirmoy Datta Consultant (DDF) Latif Bawany Jute Mills Ltd. Adamjee Court (Annex-1) Motijheel C/A, Dhaka-1000 Tel.: 9558198 Mob.: 01712197861 E-mail: jyotirmoydatta01@yahoo.com Md. Abul Hossain General Manager (Project Head) Latif Bawany Jute Mills Ltd. Demra, Dhaka. Tel.: 7500006, 7500009/201 Mob.: 01199-868289 Fax: 88-02-7500006 UMC Jute Mills Ltd. Md. Shafiqul Hai Dy. General Manager (Project Head) UMC Jute Mills Ltd., Narshindi Tel.: 9463281 (Office) Mob.: 01198-100673 Fax.: : 88-02-9462468 Karim Jute Mills Ltd. Md. Sazzadur Rahman Manager (Project Head) Karim Jute Mills Ltd. Demra, Dhaka. Tel. : 7500011, 7500020 Mob.: 01556-315331 | Bangladesh Jute Mills Corporation Major General Humayun Khaled, psc Chairman Bangladesh Jute Mills Corporation¦ Adamjee Court (Annex-1) Motijheel C/A, Dhaka-1000 Tel.: 88-02-9565514, 9553364. Fax: 88-02-9567508, 9564740 Mob.: 01755-639417 E-mail: khd732@yahoo.com bjmc.bd@gmail.com Website: www.bjmc.gov.bd Md. Abu Sayed Director (Marketing & RQC) Bangladesh Jute Mills Corporation Adamjee Court (Annex-1) Motijheel C/A, Dhaka-1000 Tel.: 9565519 Fax: 88-02-9567508, 9564740 E-mail: masayed1954@gmail.com bjmc.bd@gmail.com Latif Bawany Jute Mills Ltd. Jyotirmoy Datta Consultant (DDF) Latif Bawany Jute Mills Ltd. Adamjee Court (Annex-1) Motijheel C/A, Dhaka-1000 Tel.: 9558198 Mob.: 01712197861 E-mail: jyotirmoydatta01@yahoo.com Md. Abul Hossain General Manager (Project Head) Latif Bawany Jute Mills Ltd. Demra, Dhaka. Tel.: 7500006, 7500009/201 Mob.: 01199-868289 Fax: 88-02-7500006 |
| 2 | Private Jute Mills | Private Jute Mills Janata Jute Mills Ltd. Najmul Huq 7 Gulshan Avenue (7th floor) Janata Jute Mills Ltd. Gulshan-1, Dhaka-1212 Bangladesh Tel.: 9888698 Mob.: 01199-802095 Fax: 88-02-9881027, 9888419 Md. Mahmudul Haque Deputy Managing Director (DMD). Janata Jute Mills Ltd. 7 Gulshan Avenue (7th floor) Gulshan-1, Dhaka-1212 Bangladesh Tel.: 9888698, 9351224 Mob.: 01199-802095 Fax: 88-02-9888419, 9881027 |
| 3 |  | Sonali Aansh Industries Ltd. Md. Nurul Islam Patwary Chairman Sonali Aansh Industries Ltd. Lal Bhaban (1st Floor) 18 Rajuk Avenue, Motijheel C/A, Dhaka-1000, Bangladesh Tel.: 9556261 Fax: 88-02-9562076 E-mail: sonali@bol-online.com |

###### For further details, please contact

National Jute Board (NJB)

Project Management Unit

75C, Park Street, 6th Floor

Kolkata – 700 016

Phone No. (033) 2226 7534, (033) 4064 6316

64995824 / 25 / 26 / 27 /28 / 33 / 34

Fax NO. (033) 2226 7535

E-mail: cfcijsg21@gmail.com / jutegeotech@gmail.com

Website: www.jutegeotech.com

Indian Jute Mills Association (IJMA)

6, Netaji Subhas Road, Kolkata : 700 001

Phone :+(91)-(33)-22209918, 22314535, 22300742

Fax : 4001-4217 ; 2231-3836

Email: ijma@ cal2.vsnl.net.in

Jute Diversification Promotion Centre (JDPC)

Dhaka, Bangladesh,

145 Monipuri Para, Near Farmgate,

IJSG Bhaban, Tejgaon,

Dhaka – 1215, Bangladesh

Phone: (+880-2) 9145511

PABX: (+880-2) 9125581-5, Ext – 120

Fax: (+880-2) 9121523

E-mail: <edjdpc@yahoo.com>,

Bangladesh Jute Mills Corporation

Adamjee Court (Annex-1)

Motijheel C/A, Dhaka-1000

Tel.: 88-02-9565514, 9553364.

Fax: 88-02-9567508, 9564740

Mob.: 01755-639417

E-mail: khd732@yahoo.com, bjmc.bd@gmail.com

Website: www.bjmc.gov.bd

| Common Fund for Commodities Willemshuis ׀Stadhouderskade 55 1072 AB Amsterdam The Netherlands Telefax: (31 20) 676 0231 Internet : www.common-fund.org | International Jute Study Group 145 Monipuri Para ׀ Near Farmgate ׀ Tejgaon Dhaka 1215 ׀ Bangladesh Ph.: (880-2) 9125581-5 (5 Lines) Fax : (880-2) 9125248-9 ( 2 Lines) website: www.jute.org |
| --- | --- |
| Jute Diversification Promotion Centre 145 Monipuri Para ׀ Near Farmgate ׀ Tejgaon Dhaka 1215 ׀ Bangladesh Ph.: 88-02-9145511, 9125581-5 (exchange) Fax : 88-02-9121523 Email: ed@jdpc.gov.bd |
| National Jute Board (PEA) Head Office : 3A & 3B, Park Plaza ׀ 71 Park Street ׀ Kolkata 700 016 E : jute@njbindia.in ׀ W: www.jute.com Project Office: 75C, Park Street ׀ 6th Floor ׀ Kolkata 700 016 T : (033) 2226 7534 / 4064 6316 / 64995824/25/26/27/28/33/34 ׀ F : (033) 2226 7535 E: cfcijsg21@gmail.com ׀ jutegeotech@gmail.com ׀ W: www.jutegeotech.com |